## Slide 1
部门：工艺设备
主讲人：孔伟鑫
2021年6月11日
DIFF Process and Equipment Introduction

## Slide 2: diffusion
Diffusion
Furnace: LPCVD, Ox Growth, Anneal
IMP/RTP: implant, Ox growth, Anneal
Semiconductor - Diffusion
Wafer
Oxide
Furnace:
Screen oxide
dopant
Implant:
Ion doped

## Slide 3: Furnace
Chamber Temperature
Wafer
Temperature
Gas Flow Pressure
Boat Position
Load | Raise | Pump | Temp. | Pump | Press. | Si3N4 | Pump | N2 | Lower | Unload
Wafer | Tower | Down | Stab. | Down | Stab. | Dep. | Down | Vent | Tower | Wafer
Furnace – Process Overview

## Slide 4: Furnace
Furnace - LPCVD Process
Oxide(SiO2)-TEOS oxide
Nitride(SiN): 3 SiH2Cl2 + 4 NH3 → Si3N4 + 6HCl + 6H2
Polysilicon(Poly-Si):SiH4(g) → Si(s) + 2 H2(g)

## Slide 5: Furnace
Wet Ox: H2 + O2 → H2O; Si + 2H2O → SiO2 + 2H2
Furnace – Oxidation Process
Dry Ox: Si + O2 → SiO2

## Slide 6
Furnace – N2 anneal
Furnace
修复晶格
提高均匀性
提高致密性

## Slide 7: Furnace
Furnace – H2 Anneal
H
H
Si
SiO2
Poly结晶
修复晶格

## Slide 8
Furnace – Equipment Overview
Furnace

## Slide 9
Furnace – Formula(SiN)
Furnace

## Slide 10: Furnace
Shutter
Furnace- Formula
Load port：FOUP 进出机台的地方
FIMS port：Wafer Charge and Discharge 处 Stage：机台存放FOUP 的地方
Carrier Transfer：把FOUP: load port – stage or
Load port – FIMS port
Wafer Transfer：Wafer FIMS port -> boat Boat Elevator：控制Boat上升下降
Shutter：当Boat下来, 避免Process chamber热散失 Reactor：Process chamber
Heater Chamber：加热区 Gas Exhaust：排放气体管线
Gas Unit：气体管线收集区

## Slide 11: Furnace
BTM TP Heater
BTM sub Heater
TOP sub Heater
TOP Spiral Heater
TOP-SP
MAIN
BTM-S
TOP-S
Main Heater
BTM-TP
Exhaust Vent
Furnace- Formula Heater

## Slide 12: Furnace
Furnace - TEL Indy(TEOS/SiN/ oxidation)
Carrier transfer
Carrier storage
Load Port
FIMS Port
Boat Elevator
Auto Shutter
Wafer Transfer Pedestal
Second Storage
Boat Storage
Transfer
Boat
Wafer Counter

## Slide 13: Rapid thermal process
RTP – Comparison with Furnace
RTP
Furnace

## Slide 14
Temperature probe
Wafer
Process Gases
Lamp
reflector
Rapid thermal process
RTP – chamber structure(AMAT)

## Slide 15: Top Lamps
Bottom
Lamps
Wafer
RTP – chamber structure(Mattson)
Rapid thermal process

## Slide 16: Rapid thermal process
RTP – Process & Equipment
Process
Rapid Thermal Anneal(RTA)
Rapid Thermal Oxidation(RTO)
Rapid Thermal Nitridation(RTN)
Hardware
Applied Centura (ISSG)
Applied Vantage (RTA/RTO)
Mattson Helios(RTA)

## Slide 17
RTP – RTA
Rapid thermal process

## Slide 18: Rapid thermal process
H2 + O2 → 2OH
H2 + OH → H2O + *H
O2 + *H H2 + *O
OH + *O
OH + *H
Reaction Mechanism
H2(g), O2(g)
ISSG :In-Situ Steam Generation
better leakage properties,gate oxide integrity,and reliability over furnace oxidation techniques
at high temp and low pressure, a mix of water vapor, OH
radicals, O radical and other species is formed at wafer surface
RTP - RTO
Dry Ox: Si + O2 → SiO2
Wet Ox(ISSG): H2 + O2 → H2O ; Si + 2H2O → SiO2 + 2H2

## Slide 19: Rapid thermal process
NO | LAMP SiO2 Silicon | — Electron + N ion N radical Self bias |  | + － + | SPA — Plasma + － － + SiO2 Si | － + － | +
RTP - Nitriding
RTN & SPA

## Slide 20: Rapid thermal process
RTP – Nitrogen distribution

## Slide 21: Rapid thermal process
RTP – Hardware introduction
① AMAT （Centura/Vantage）机台
旋转方式：磁悬浮承载，240rpm；
测温方式：下方装有7根pyrometer；
加热模式：上部加热（409个灯泡，15个区域）；
可以调节灯泡的温度来控制process的区域温度。

## Slide 22: Rapid thermal process
RTP – Hardware introduction
Centura机台：Load port、Factory interface、Load lock、
Mainframe、Process chamber

## Slide 23: Rapid thermal process
RTP – Hardware introduction
Vantage机台：Load port、Factory interface、Process chamber

## Slide 24: Rapid thermal process
RTP – Hardware introduction
② Mattson Helios 机台
旋转方式：气动控制，90rpm ；
测温方式： pyrometer ；
加热方式：双面加热（上下方各有28个Lamps加热）。

## Slide 25: Rapid thermal process
RTP – Hardware introduction
Mattson机台：Lord port、Handler Module、Chamber、Cooling station

## Slide 26
SiO2 |  | 
Si |  | 
Ion implantation
Thermal diffusion
Doped region
PR
Si
Implantation
Implant – thermal diffusion v.s. implantation

## Slide 27: Implant – beam line overview
Ion
Source
Vacuum
Pump
Analyzer Magnet
Beam
Line
End Analyzer
Vacuum Pump
Wafers
Plasma Flooding System
Post Acceleration
Electrode
Extraction Electrode
Suppression Electrode
ion
Si

## Slide 28
Implant – bombard energy
Implantation

## Slide 29: Implantation
Implant – dopant distribution
Rp

## Slide 30: Implant – Shadow effect
Polysilicon
Doped Region
Substrate
Shadowed Region
Ion Beam

## Slide 31
Implant – Channel effect
Channeling Ion
Lattice Atoms
Collisional Ion

Wafer Surface

## Slide 32: IMP机台类型和构造
① 根据功率分类(目前我们公司的机台)
中电流机型：VIISTA 810EHP（AMAT）
  能量：2~300KeV；剂量范围：1E11~1E15 ion/cm2
高电流机型：HCS （AMAT）
  能量：0.5~80KeV；剂量范围：2E13~1E17 ion/cm2
高能量机型：HE3（AXCELS）
  能量：40~4600KeV；剂量范围：5E11~1E15 ion/cm2
② 根据生产方式分类
单片晶圆
批量生产
Implant简介及机台构造
Implant – Hardware introduction

## Slide 33: Implantation
Implant – Hardware introduction
③ 机台的主要组成部分
束流计测
（FARADAY)部
质量能量分析部
硅片搬送部
离子源部
Ion Source
其他支持系统
通过加热、电离、碰撞的过程将气体、固体杂质离子化
通过磁场筛选出目标离子
通过中和电子的数量测量离子束流
机械传送

## Slide 34
感 谢 聆 听