## Slide 1
ACM Tools
ACM Research, Inc.
2021-5-13

## Slide 2
ACM 12寸WET设备
 |  | 应用 | 类型 | New or Used | 型号 | 化学药液
WET | 1 | 前段晶圆颗粒清洗 | Single | New | Ultra C s II (Single 8 Chambers) | CO2DIW
WET | 2 | 后段晶圆颗粒清洗 | Single | New | Ultra C s II (Single 8 Chambers) | CO2DIW
WET | 3 | 背面刻蚀和清洗去胶 | Single | New | Ultra C b (Single 4 Chambers) | 2CH: HNO3/HF, CO2DIW 2CH: DSP+, CO2DIW
WET | 4 | Thin wafer | Single | New | Ultra C b (Single 2 Chambers) | SPIN D, SPIN E, DHF, DIW

## Slide 3
1.Scrubber/Bevel clean(Single)
Ultra C 318 Basic Feature
W*L*H= 2.242m*2.315m*2.85m
Process Application: Scrubber/Bevel Clean
Model: Ultra C 318
Chamber Count: 8ea, 4 chamber N2 spray DICO2 + 4 chamber Brush
Robots: One index robot with 2ea arms, one process robot with 2ea arms
Chuck: Mechanical&Vacuum Chuck, with conductive pin
Clean: Wafer front side, backside, Bevel
Physical Assist Clean: N2 spray DICO2/DIW, Brush
Dry Method: Spin dry; N2 spin dry
Chemical Configuration:
Particle:
  <20ea@40nm, Bare Si
Metal contamination (ICPMS): <5E9 atm/cm^2
Etch Rate Uniformity(%): N/A
Chemical | Front | Back | Temp. | Conc. | Reclaim/to Drain
DICO2/DIW | v | v | RT | 0.1MΩ*cm | to Drain
N2 Spray DICO2/DIW | v |  | RT | 0.1MΩ*cm | to Drain

## Slide 4
1.Scrubber/Bevel clean(Single) Configuration

## Slide 5
3F
Ultra C 318
W*D*H= 2.35*6.125*2.85
2F
2.5F
1.Scrubber & Sub unit Layout Overview
W*L*H=
2.242m*2.8034m*2.85m

## Slide 6
1.Frontside Clean Chamber Config
Bevel Brush
N2
Nozzle1:Nano CO2/DIW
Swing Arm1
Swing Arm3
Swing Arm2
Vacuum Chuck
Fix Nozzle
Nozzle1:CO2 DIW
Wafer Get & Put
Nozzle2:CO2/DIW
Nozzle2:CO2 DIW
Chamber Nozzle Configuration | 
Arm 1 | Bevel Brush
Arm 2 | NANO CO2 DIW, CO2 DIW
Arm 3 | N2
Back Side
Nozzle1:CO2 DIW
Nozzle2:N2
Exhaust
NANO CO2 DIW
FFU
Swing Arm2
CO2 DIW
Fix DIW 1& 2
CO2 DIW Drain
Backside Nozzle1:CO2 DIW
Backside Nozzle2: N2
Swing Arm3
N2
Bevel Brush
Swing Arm1Arm1
Nozzle&drain configuration
6

## Slide 7
1.Backside Clean Chamber Configuration
Backside Brush
N2
Nozlzle1:NANO CO2/DIW
Swing Arm1
Swing Arm3
Swing Arm2
Fix Nozzle
Nozzle1:CO2 DIW
Nozzle2:CO2/DIW
Nozzle2:CO2 DIW
Chamber Nozzle Configuration | 
Arm 1 | Backside Brush
Arm 2 | NANO CO2 DIW, CO2 DIW
Arm 3 | N2
Nozzle&drain configuration
Back Side
Nozzle1:CO2 DIW
Nozzle2:N2
NANO CO2 DIW
FFU
SW2
Exhaust
CO2 DIW
Fix DIW 1& 2
Common
Drain
Backside Nozzle: N2
SW3
N2
Backside Brush
SW1
7

## Slide 8
2. Backside Clean + DSP Clean
Process Application: Backside Clean + DSP Clean
Chamber Count: 4ea
Robots: One robot with two arms
Chuck: Bernoulli chuck
Dry Method: Spin dry; N2 spin dry
Chemical Configuration:
Particle:
  Wafer front side: 0.12um ≤ 5ea; 0.060um≤ 20ea ;0.040um ≤ 40ea
Metal contamination (ICPMS): ≦1E+10 (atoms/cm2)
Etch Rate Uniformity(%): <3%, TOX
W*L*H=2580mm*2460mm*2410mm
Chemical | Front | Back | Temp. | Conc. | Reclaim/to Drain
HNO3/HF | v |  | R.T~30℃, 23±0.5 | HF:HNO3=1:10 -1:100 | Reclaim
CO2_DIW/DIW | V |  | RT | 0.2MΩ*cm | to Drain
DSP | v |  | R.T~30℃, 23±0.5 |  | Reclaim

## Slide 9
Inner Shroud up, liquid flow into the inner tray, for HNO3/HF reclaim and HNO3/HF drain
Inner Tray
Outer Tray
Common Drain
Inner shroud down, liquid flow into the outer tray, N2 dry and pre and post rinse drain.
HNO3/HF Reclaim
HNO3/HF Drain
Swing arm1
Swing arm3
Nozzle1: N2
Nozzle1: HNO3/HF
Nozzle1: DIW CO2
Swing arm2
HNO3/HF rinse Drain
2. Backside Clean Chamber Configuration
Chamber 1-2

## Slide 10
2.Chamber Configuration (DSP)
Swing arm1
Swing arm2
Swing arm3
Nozzle1: N2
Nozzle1: DSP+
Inner Shroud up, liquid flow into the inner tray, for DSP+ reclaim and drain.
Inner Tray
Outer Tray
Common Drain
Inner shroud down, liquid flow into the outer tray, N2 dry and pre and post rinse drain
Nozzle2: CO2 DIW/DIW
DSP+ Reclaim
DSP+ Drain
DSP+ Post rinse Drain
Chamber 3-4

## Slide 11
4. Thin Wafer Backside Clean (Single)
Process Application: Thin wafer backside Si wet etch
Chamber Count: 2ea(4chamber platform with 2ea chamber mounted)
Robots: Bernoulli arm
Chuck: Bernoulli chuck
Dry Method: Spin dry; N2 spin dry
Chemical Configuration:
Si thickness monitor unit: Installed
Particle:
  Si-Etchant - DHF<50ea@120nm
Metal contamination (ICPMS): <5E10 atm/cm^2
Etch Rate Uniformity(%): <3%, TOX
Wafer thickness: 200um or 200um Taiko wafer or bonding wafer
Wafer warpage: +/-5mm
Bath | Front | Back | Temp. | Conc. | Reclaim/to Drain
SPIN-E or SPIN-D | v |  | 30℃-60℃ |  | to reclaim
DHF | v |  | 23±1℃ | 1:10-1:50 | to reclaim
DIW | v |  | RT |  | to Drain
W*L*H=2580mm*2460mm*2410mm

## Slide 12
robot
Chamber D (不安装)
Plumbing CD
Plumbing AB
Chamber A
Chamber C (不安装)
Chamber B
N2 gas panel
loadport
EE panel
Main Plumbing
4.Thin Wafer Backside Clean (Single)
Ultra C b Basic Feature

## Slide 13
4.Chamber Configuration
HF Reclaim
HF Drain
Middle Tray
Inner Tray
Outer Tray
Common Drain
Si Etchant 1 Reclaim
Si Etchant 1 Reclaim
Swing arm1
Swing arm3
Nozzle1: N2
Nozzle1: Si Etchant
Nozzle1: DIW
Swing arm2
Nozzle2: DHF

## Slide 14
4.Thin Wafer Robot Transfer-Bernoulli arm
FOUP
Weight stage
Chamber
Weight stage
FOUP
Flip
Flip
Bernoulli arm
Bernoulli arm
Bernoulli arm
Bernoulli arm
Wafer Transfer Schedule

## Slide 15
Chuck pin
Advantage
Six Clamp pins: For preventing wafer horizontal movement during wafer
- each clamp pin is driven by an independent cylinder to move inwardly to hold wafer or outwardly
to release wafer
- 6 clamp pins are divided into two groups disposed alternately. During process, the two group alternately
holding/releasing wafer, so the wafer edge can be cleaned
Safety
Edge clean
Clamp pin
Bernoulli N2 holes
4.Chuck Configuration

## Slide 16
ACM
L Company
Chuck comparison
Same Points
Application of Bernoulli Effect for Wafer floating, no touch between wafer Frontside and chuck
Different Points
ACM：Two types of N2 holes
– First type : inclined with certain angle, distributed on chuck periphery for provide Bernoulli effect source
– Second type : perpendicular, distributed around chuck center for wafer lifting
L：One type of N2 holes
– with certain angle distributed on chuck periphery for provide Bernoulli effect source
4.Chuck Configuration